Supporting Information

Magnetic functionalized graphene: An efficient and solid acid catalyst for the synthesis of highly functionalized pyrroles under ultrasound irradiation

Sodeh Sadjadi *

Radiation Application Research School, Nuclear Science and Technology Research Institute, Tehran, Iran, P. O. Box: 14399-51113.

*Corresponding author’s email: sadjadi.s.s@gmail.com

Figure S1. The XRD pattern of rGO-hydroxamic acid/Fe3O4 catalyst.

Figure S2. The FTIR spectrum of rGO-hydroxamic acid/Fe3O4 catalyst.

Table S1. The quantitative results of EDS analysis.

| Element | Weight % | Atomic % |
| --- | --- | --- |
| C | 29.56 | 45.83 |
| N | 7.71 | 10.25 |
| O | 27.69 | 32.23 |
| Fe | 35.04 | 11.68 |